## Slide 1: NAPLIFE Collaboration
Nanoparticle doping of fusion targets
Dr. Attila Bonyár
bonyar@ett.bme.hu
Budapest, 2022.05.18.

## Slide 2: Speaker Introduction
Attila Bonyár is an associate professor at the Department of Electronics Technology at Budapest University of Technology and Economics.
He has two M.Sc. degrees in electrical engineering and biomedical engineering and Ph.D + habilitation in electrical engineering.
His research activities are focused on the development of optical, affinity type biosensors, utilizing low-dimensional nanomaterials, plasmonics and nanometrology (AFM).
Chair of the IEEE Hungary&Romania EPS&NTC (Electronics Packaging Society and Nanotechnology Council) joint chapter since 2019.
IEEE EPS/NTC Nanotechnology/Nanopackaging Technical Committee chair since 2022, co-chair since 2019.
IEEE NTC Region 8 Chapters Coordinator.

## Slide 3: Agenda
Introduction of the NAPLIFE Collaboration and our work group
Considerations for target fabrication
Nanocomposite target preparation – results
  Tuning of plasmonic properties
  Controlling the layer thickness
Conclusions

## Slide 4: 1. Introduction of the NAPLIFE project
Theoretical group (modelling, simulations)
Target fabrication group (nanocomposite preparation, measurements)
Laser group
(Target irradiation)
Analytical group
(Effect detection)
Target properties
Target
Irradiated target
Target performance
Material properties
Nano-Plasmonic Laser Inertial Fusion Experiment Collaboration

## Slide 5
1. Introduction of the Target Fabrication Group
Dr. Bonyár Attila
Associate Professor
Alexandra Borók, Shereen Zangana, Rebeka Kovács
PhD Students
Coordination, target fabrication from nanocomposite, optical measurements, etc.
Dr. Szalóki Melinda
Assistant Professor
Dr. Petrik Péter
Senior Research Fellow, Head of Laboratory
Optical measurements (ellipsometry), transmission electron microscopy (Dr. Zsolt Fogarassy)
Polymer chemistry, doping of nanomaterials, nanocomposite preparation

## Slide 6: 2. Considerations for the target
Number of layers: n=10
d1=d2=…=dn= 2 mm
D = sum(d) = 20 mm
rn: concentration of the nanoparticles in the layers.
.
.
.
.
.
.
.
.
.
d1, r1
d2, r2
d3, r3
dn, rn
Laser beam
Laser beam
20 µm
Target thickness [µm]
Number of nanoparticles [-]
The planned target is a model material, where the density of the nanoparticles (and thus the absorption) in controlled in layers.
Calculations from the Theory Group
Target schematics considering two-sided irradiation
Calculations from the Theory Group
Wavelength [nm]
Absorption cross-section [10-14 m2]

## Slide 7: 2. Considerations for the target
Boundary conditions (requirements):
The continuous nanoparticle distribution will be approximated with layers of constant nanoparticle densities.
The layer thickness needs to be controlled (approx. 2 µm).
The absorption peak should be at 795 nm.
The nanoparticle density should be controlled, aggregation should be avoided.
Multiple particle types should be tested (e.g. nanorods, nanoprisms, core-shells…)
Questions to be answered:
What matrix material should we use?
How to control the layer thickness and build layers on top of each other?
How to synthetize nanoparticles with various shape and size?
How can we control the plasmon absorption peak of the final target material?

## Slide 8: 2. Considerations for the target
The selected polymerization method is photopolymerization:
Works with thin layers (see microtechnology resists e.g. SU-8).
Fast polymerization (a couple of minutes).
Polymerized layers are stable in organic solvents.
Layers can be built on each other.
The selected polymer is UDMA (urethane dimethacrylate) with TEGDMA (Triethylene Glycol Dimethacrylate) dilution monomer, CQ (Camphorquinone) photoinitiator and EDAB (ethyl 4-dimethylaminobenzoate) co-initiator, which is a well-known mixture in dentistry.
Emission spectrum of a standard blue-light lamp
Emission [-]
Wavelength [nm]
Acrylate resin in cavity

## Slide 9: 3. Target preparation – layering technologies
Advantages / Disadvantages:
+ Precise control over layer thickness.
Viscosity has to be controlled.
The polymerisation is sensitive to oxygen.
réteg
képzése
felcseppentés
elvékonyítás
szárítás, polimerizáció
Nitrogen flow
Blue light lamp
Sample
(Source: Rodrigo Perez Gartia)

## Slide 10: 3. Target preparation – layering technologies
Advantages / Disadvantages:
+ Oxygen is not an issue.
+ Optically perfect, smooth layer.
Viscosity has to be controlled.
The thickness is hard to be controlled in the µm range.
Future improvement:
Multi-levelled frame created with thin film technology.
Polymerization during mechanical shaping between glass slides
Polymer
Glass slide
Glass slide
Light source
Spacer
1
2
3

## Slide 11: 3. Target preparation – controlling the layer thickness
Plasma etching of the UDMA-TEGDMA material
High-power plasma reactor using focused H plasma (left) and defocused Ar plasma (right).
Low-pressure plasma chamber using O2 (left) and Ar+Hr (right) as process gases for plasma generation.
A reproducible etching rate of 80 nm/min was found in O2 plasma at 300 W power, 0.3 mbar pressure.

## Slide 12: 3. Target preparation – layering technologies
Ellipsometry
Woollam M-2000DI
Wavelength [nm]
Wavelength [nm]
n
k
Psi
Delta
The measured Psi-Delta and the fitted model
The complex refractive index (1 µm layer)

## Slide 13: 3. Target preparation – nanoparticle synthesis
Gold nanoparticles from HAuCl4 solutions
(Source: Nguen et al, 2011)
HAuCl4 salt crystals
Nanoparticle synthesis
Size- (left) and size-controlled (right) growth
Reduction
Growth direction

## Slide 14: 3. Target preparation
Wavelength [nm]
Normalized extinction [-]
Normalized absorption [-]
Wavelength [nm]
Absorption [O.D.]
Wavelength [nm]
Absorbance measurements with optical spectroscopy
Absorption spectra of 25 × 75 nm gold nanorods. Left: manufacturer. Right: own measurement
NanopartzTM
Illustration of the optical (dip) probe measurement setup (right)
Own measurement
Peak (water): 695 nm
FWHM: 105 nm
FWHM

## Slide 15: 3. Target preparation – nanoparticle size control
Transmission electron microscopy (TEM)
100 nm
NanopartzTM datasheet
Own measurements (Fogarassy Zsolt, ELKH-EK-MFA)
Nominal values from the manufacturer: 25 × 75 nm (±10 %)
Own measurements:
Average (deviation) for 28 nanoparticles: 26 (1.65) × 76 (7.97) nm

## Slide 16: 3. Target preparation – nanoparticle size control
Transmission electron microscopy (TEM)
A new direction: gold and silver nanoprisms, synthetized in Jena (Germany).

## Slide 17: 3. Target preparation – nanoparticle phase transfer
Water + nanoparticles (top)
Organic solvent (bottom)
Organic solvent + nanoparticles (bottom)
Water (top)
Importance of the molecular layer covering the nanoparticles (capping)
Phase transfer: changing CTAB to alkanethiol
Wavelength [nm]
Extinction [-]
It is important to make the nanoparticles soluble in the polymer matrix, to avoid aggregation and to ensure uniform distribution.
Solubility is defined by the molecular capping.
Illustration of particle aggregation

## Slide 18: 3. Target preparation – particle distribution control
Investigation of the embedded particles with TEM
Density of nanorods: 9-20 db mm-3
Calculated from stock solution: 2 db mm-3
Sn NP !

## Slide 19: 3. Target preparation – particle distribution control
Investigation of the absorbance with optical spectroscopy
Nanoparticle aggregation starts at 3.8x1012 mL-1
Full spectrum of the nanocomposite (25x85 nm rods)
VIS spectrometer
NIR spectrometer
Wavelength [nm]

## Slide 20: 3. Target preparation – fine tuning the absorption band
Refractive index sensing with nanoparticles
Wavelength [nm]
Absorption [A.U.]
n1
n2
Bulk refractive index sensitivity (RIS):
Source: Springer, Nanoplasmonic Sensors (2012)
Illustration: gold nanodiscs on glass in water and in air
n1 = 1
n2 = 1.33

## Slide 21: 3. Target preparation – fine tuning the absorption band
Heat treatment was used to shift the absorption band – control with time and temperature
Wavelength [nm]
Time [min]
Normalized absorption [-]
Absorption peak position [nm]
25x75 nm nanorods

## Slide 22: 3. Target preparation – fine tuning the absorption band
The charts can be used to control the absorption in a wide range
25x85 nm nanorods
Absorption peak position [nm]
Wavelength [nm]
Time [min]
Normalized absorption [-]

## Slide 23
Conclusions
“Take-home messages”
Our current target is a model material made of a nanocomposite (doped polymer).
Layering technologies are used to realize pre-defined nanoparticle distributions along the target’s thickness.
Nanoparticle synthesis and doping are controlled with optical spectroscopy and TEM.
A method based on thermal treatment was developed to fine tune the plasmon absorption band of the nanocomposite.

## Slide 24
Acknowledgements
For the colleagues in the sample preparation group (Dr. Szalóki Melinda, Dr. Petrik Péter, Borók Alexandra, Kovács Rebeka, Shereen Zangana).
Whole NAPLIFE collaboration.
NKFIH, ELKH for financial support.

## Slide 25
Acknowledgements
This work was partially supported by Nanoplasmonic Laser Fusion Research Laboratory project financed by the National Research and Innovation Office (NKFIH-468-3/2021) and by the Eötvös Lóránd Research Network (ELKH), Hungary. The research reported in this paper and carried out at the Budapest University of Technology and Economics has been supported by the NRDI Fund (TKP2020 IES, Grant No. BME-IE-BIO) based on the charter of bolster issued by the NRDI Office under the auspices of the Ministry for Innovation and Technology.