## Slide 1: Femosecond LIBS experiments from polymer targets
Rácz Péter
NAPLIFE collaboration
Wigner Research Centre for Physics

## Slide 2
Laser Induced Breakdown Spectroscopy (LIBS)
LIBS: is a chemical analysis technology that uses a short (fs- ns) laser pulse
to create a micro-plasma on the sample and based on atomic emission spectroscopy
to measure elemental composition.
Sample preparation-free measurements
It can be used on any material, whether solid,
liquid, or gas, foil
Broad elemental coverage, including lighter
elements, such as H, He Li, C, N, O, Na, and Mg,
and heavy metallic elements too
https://appliedspectra.com/technology/libs.html

## Slide 3
Field of applications:
Food science application: Measurement essential (Mg, Ca, and K) and
toxic elements (Pb, Hg, St, Mn)
Study of geological samples: identification of minerals
Investigation of biological samples
Pollution Monitoring
Industrial application: in chemical industry material identification during manufacturing
processes, in semicunductor industry used in semiconductor wafer and coating
characterization and for quality control.
The most appropriate applications of LIBS are in the nuclear and chemical industry,
where quantitative or qualitative remote analysis, without any physical contact with the sample,
is preferred.
Further perspective in space exploration (for example on Mars rover)
Applications of LIBS

## Slide 4
Applied laser systems for LIBS
ns pulsed laser:
fs pulsed laser:
-Nd:YAG Laser System:
wavelength: 1064 nm, 532 nm
pulse duration: 5–10 ns
typical pulse energy: 10-300 mJ
-The ruby laser:
wavelength: 693 nm
pulse duration: 20 ns;
low ablation threshold,
improved spatial resolution for 3D mapping
applications,
small ablated mass, and reduced sample damage
Ti:Sapphire chirped-pulse amplifier (CPA):
wavelength: 800 nm
pulse duration: 30–100 fs
typical pulse energy: 10-50 mJ
Advantages of fs-LIBS:

## Slide 5
Laser Ablation Process
Continuum light emmission
< 0.1 ~ 0.3 µsec
Sergio Musazzi, Umberto Perini: Laser-Induced Breakdown Spectroscopy, Springer Berlin 2014
Emission of discrete atomic lines at later times (~ 1 µsec).
Approximate time scales of nanosecond and femtosecond energy absorption and
laser ablation along with various processes happening during and after the laser pulse is given

## Slide 6
Timescales
τ< 0.1 ~ 0.3 µsec
Plasma temperature 10000-20000 K
Continuum light emmission (Recombinations, ion lines)
τ ~ 1 µsec
Plasma temperature 1000-2000 K
Emission of discrete atomic lines

## Slide 7
Instrumentation for LIBS
Plasma
Jet
Light collecting optics

## Slide 8
Femtosecond Ti:Sapphire chirped-pulse amplifier
Pulse energy: max. 25-30 mJ
Pulse length min. 40 fs
Central wavelength 795 nm
Repetition rate: 10 Hz
Max Peak Power ca. 1 TW
Focused max. peak intensity approx. 1018 W/cm2
Coherent Hidra-25:
Applied laser system

## Slide 9
Experimental Setup
Laser pulse
Spectrometer:
LTB Demon spectrometer
(Double Echelle Monochromator)
Detector : ICCD
Wavelength range: 190-900 nm
Spectral resolution: 2.5-12 pm
Simultaneous inspection range: 3 nm
Laser pulse
Light collecting optics
Environme conditions:
In vacuum (10-5 mbar)
Ar gas ~2-5 mbar for higher level signal

## Slide 10
LIBS measurements from copper target
Signal optimisation experiment

## Slide 11
Stability of the plasma light intensity
10 shots into the same sample position
Every shot into a new sample position
Quite stable signal from plume

## Slide 12
UDMA (urethane dimethacrylate), C23H38N2O8
Polymer targets
1. type
UDMA:TEGDMA mixture (3:1)
TEGDMA (triethylene glycol dimethacrylate), C14H22O6
Bare polymer
Nanocomposite
Nanocomposite: UDMA:TEGDMA mixture (3:1) + AU nanorods
2. type
Size of AU nanorods: 85 nm x 25 nm, Plasmonic resonance to 795 nm
3. type:
UDMA:MMA-D mixture (3:1)
Deuterated samples
MMA-D (Methyl methacrylate): C5D8O2
=0,32
See details in Attila Bonyár presentation
Used in in dental medicine

## Slide 13
Measurements from deuterated sample
Single measurement
3 mj, Ar 2 mbar τd=0,9 µs
Average of 20 measurement
3 mj, Ar 2 mbar τd=0,9 µs
Single measurement
3 mj, Ar 5 mbar
τd=0,9 µs
Average of 20 measurement
3 mj, Ar 5 mbar τd=0,9 µs
Balmer α lines: hydrogen 656.28 nm and deuterium 656.11 nm.
UDMA:MMA-D mixture (3:1)

## Slide 14
Single measurement
25 mj, Ar 2 mbar τd=0,9 µs
Single measurement
25 mj, Ar 2 mbar τd=0,8 µs
Measurements from bare polymers and nanocoposite samples
Nanocomposite: UDMA:TEGDMA mixture (3:1) + AU nanorods
Preliminary results

## Slide 15
Bare Polymer: UDMA:TEGDMA mixture (3:1)
Nanocomposite: UDMA:TEGDMA mixture (3:1) + AU nanorods

## Slide 16
Summary
LIBS experiment from deuterated polymer samples
We can detect deuterium with LIBS method
Measurements from nanocoposite targets (UDMA:TEGDMA mixture (3:1) + AU nanorods
Deuterium signal also present in this type of targets
Possible explanation: deuterium production
Next step: incrising the signal
Thank you for your attention!

## Slide 17
Norbert Kroó, Tamás Biró, László Csernai, Miklós Veres, Márk Aladi,
Miklós Kedves, Archana Kumári, Judit Kámán, István Rigó
Wigner Research Centre for Physics
Department of Electronics Technology, BME
Attila Bonyár, Alexandra Borók
Gábor Galbács
Department of Inorganic and Analytical Chemistry,
University of Szeged

## Slide 20
1.9x1012 pice/ml | 0.1236 m/m%
Concetration