## Slide 1
Hard x-ray spectrograph
and
anomalous soft modes
in a-iron
Aleksandr Chumakov
European Synchrotron Radiation Facility
Nuclear Resonance beamline ID14

## Slide 2: Hungary at ESRF:
ESRF upgrade
&
COVID time
Many thanks to these people!
- for making ESRF better;
- for making ESRF famous.

## Slide 3: Thanks from Nuclear Resonance beamline ID18 (→ ID14)
Miklos Tegze
Gyula Faigel
Three dimensional imaging of atoms
with isotropic 0.5 Å resolution
PRL 82 (1999) 4847
Acquiring of holograms
requires
high beam stability
(no vibrations)
Upgrade of LN2
cooling system
of
ID18 monochromator
excellent stability
of x-ray beam,
vibration amplitude:
< 0.1 mrad (rms)

## Slide 4: Thanks from Nuclear Resonance beamline ID18 (→ ID14)
Dániel Merkel
Dénes Nagy
A three-dimensional analysis
of magnetic nanopattern formation
in FeRh thin films on MgO Substrates:
implications for spintronic devices
Appl.Nano.Mater. 5 (2022) 5516
Request to study
singe
nano-particle
New instrument
“Nanoscope”:
focusing mirror
with short focal length
sub-micron
beam size:
380 nm × 650 nm
(H × V)

## Slide 5: Thanks and news from X-ray absorption and emission spectroscopy beamline ID26
György Vankó
Hard-X-ray-Induced
Excited-Spin-State Trapping
Angew. Chem. 46 (2007) 5306
News from
Pieter Glatzel:
(ID26)
XANES:
X-ray Absorption
Near Edge Structure
HERFD-:
High Energy Resolution
Fluorescence Detected
techniques

## Slide 6: Thanks and news from material science beamline ID11
Gábor Ribárik
Burgers vector population,
dislocation types and dislocation densities
in single grains
extracted from a polycrystalline commercial-purity
Ti specimen by X-ray line-profile analysis
Scripta Materialia 63 (2010) 69
News from
Jonathan Wright:
(ID11)
Today at ESRF,
with Extremely Brilliant Source,
you can do similar studies
by an order of magnitude faster!

## Slide 7: Beamtime use by Hungary in 2022 – % by scientific area

## Slide 8: Many thanks, and we hope to see you again at ESRF!
Many thanks to you and to many others!
we hope to see you again at ESRF!

## Slide 9
Hard x-ray spectrograph
and
anomalous soft modes
in a-iron

## Slide 10: Outlook:
Motivation:
      - from monochromator to spectrograph
Hard x-ray spectrograph:
      - optical scheme
- short introduction to Nuclear Inelastic Scattering
Hard x-ray spectrograph:
      - experimental results
          - Anomalous atomic dynamics of alpha-iron.

## Slide 11: X-ray monochromator: for diffraction and for spectroscopy
fixed angle
Diffraction:
Spectroscopy:
angular scan
fixed energy
energy scan
we take good photons
we do not need others
2d
we take some photons
but we also need others
100 meV
1 meV

## Slide 12: From monochromator to spectrograph
Isaac Newton, Opticks, 1704).
position-sensitive
detector
Spectrograph: all energies at once
Dispersion:
Does not work for x rays:
- too small refraction
- big absorption
There is a way out:
- asymmetric diffraction
- dispersion amplification

## Slide 13: asymmetric reflection
symmetric reflection:
asymmetric reflection:
T. Matsushita and U. Kaminaga, J. Appl. Crystallogr. 13, 472 (1980).
bad for focusing …
Y. V. Shvyd’ko, M. Lerche, U. Kuetgens, H. D. Rüter, A. Alatas, and J. Zhao, Phys. Rev. Lett. 97, 235502 (2006).
good for dispersion!

## Slide 14: Hard x-ray spectrograph
Bad news:
- small angular range
- i.e., small energy bandwidth …
Good news:
- big dispersion,
- i.e., good energy resolution
Hard-x-ray spectrographs:
Y. Shvyd’ko, S. Stoupin, K. Mundboth, and J. Kim, Phys. Rev. A 87, 043835 (2013).
Rainbow

## Slide 15: Hard x-ray spectrograph: optical scheme
Multiple asymmetric reflections create and enhance dispersion.
X rays of different energies are directed at different angles.
Lens system focuses x rays of different energies at different vertical positions.
Small slits provides high energy resolution, availability of all beams keeps flux.
ac et al, PRL 123, 097402 (2019)

## Slide 16: Hard x-ray spectrograph: optical scheme
How to
measure:
resolution and
spectral window:
dispersion:
resolution:

## Slide 17
before coming to
experimental data:
short introduction to Nuclear Inelastic Scattering
(nuclear inelastic absorption)

## Slide 18: Nuclear resonance scattering
G  2 eV
t0  0.33 fs
E = 7.112 keV
s
e
=
26
×
10
-
20
cm
2
G = 4.7 10-9 eV
t0 = 141 ns
E = 14.412 keV
s
n
= 256
×
10
-
20
cm
2
14.412 keV
136.5
366.8
706.4
Fe
57
26
Electronic and nuclear levels:

## Slide 19: Nuclear inelastic scattering (absorption)
Energy
Absorption
detector
monochromator DE ~ 0.6 meV
0.1 ns
176 ns
time
counts
pulsed structure of
synchrotron radiation:
time gate
energy scan
14.4 keV
6.4 keV
~ few hours for sample with resonant isotope ( 57Fe )
~ a day for other samples (SiO2)

## Slide 20: Nuclear inelastic absorption
Very narrow level:
G = 4.7 neV
Very long time:
t0 = 141 ns
Time of interaction:
~105 phonon lifetimes.
Scattering is impossible:
Absorption:
ideal integration over all q-vectors
well defined
changes
with time
(averaging)
does not know
where to emit
dispersion
relations
DOS
not we, nature
no need for analyzer
much easier to get very high energy resolution

## Slide 21: Velocity distribution of vibrating atoms
57Fe nuclei
v+
v-
E = Eres (1+v/c)
Classical interpretation of Nuclear Inelastic Scattering:
monitoring velocity distribution of vibration atoms
Imagine 57Fe nuclei
in cars running on a road
Measure velocity
by Doppler effect

## Slide 22: Hard x-ray spectrograph: experimental results
ac et al, PRL 123, 097402 (2019)
Spectrograph, energy resolution = 0.11 meV
Accurately study extremely small differences:
Four samples (S) and four detectors(D):
DE = 1.5 meV
t = 0.53 ns
dE = 254(19) meV
Instrumental function
difference in energy
of optical modes for
K3MgFe(CN)6 and
(NH4)2MgFe(CN)6

## Slide 23: Hard x-ray spectrograph: experimental results
ac et al, PRL 123, 097402 (2019)
Spectrograph, energy resolution = 0.11 meV
Four samples (S) and four detectors(D):
Four
identical
samples
of alpha-iron
Anomalous soft modes
in normal ambient a-iron
Sum all spectra,
use all radiation components,
Gain both:
high energy resolution
and high flux:

## Slide 24: Alpha-iron: one of the most studied by mankind system
Minkievicz et al., PR 162, 528 (1967)
Neuhaus et al., PRB 89, 184302 (2014)
1200 B.C. – 600 B.C.
Simple BCC structure:
Lattice
dynamics:
q
ω(q)
ω = v q
sound velocity
ω(q)
VL
VT1
VT2
VL
qx
qy
qz
integrate number of states
in 3D:
n(q) ~ 4pq2
should be
a constant,
~ 1/<V3> !!!
n(ω)/ω2
known sound velocity
density of states
reduced density of states
(raw spectrum)
measurements with low resolution:

## Slide 25: Alpha-iron: now with 0.1 meV energy resolution
effect is seen in raw data
statistical uncertainty: error bars
uncertainty of subtraction of elastic peak: less than symbol size
Earlier data, measured with
the energy resolution of 0.7 meV

## Slide 26: Density of states: measured by NIS and from dispersion relations
measured by NIS
(blue dots):
complete picture
of ALL atomic displacements,
no momentum resolution
from dispersion relations
(red curves):
calculated DOS
using force constants
fitted to measured
eigen - friequences
in selected q-points
measurements with low resolution:

## Slide 27: Anomalous modes: temperature dependence
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
Minkievicz = V.G.Minkievicz et al., PR 162, 528 (1967)
Temperature dependence of the excess?

## Slide 28: Anomalous modes: temperature dependence
Life-time broadening
Excess of reduced DOS
Excess of modes increases close to T2: anharmonism?
But it changes behavior at Curie temperature: magnons?
TC
anharmonism:

## Slide 29: Possible origins:
1. Positive curvature
of T2 branch:
but: not seen by INS
2. Anharmonism:
J. Scheipers and W. Schirmacher,
Z. Phys. B 103, 547 (1997).
3. Magneto-elastic
waves
(magnon-phonons):
spin displacements
spatial displacements of atoms
harmonic
anharmonic

## Slide 30: To take home:
Hard x-ray spectrograph is possible:
- ESRF: offered to users (phonon spectroscopy)
- LCLS: in technical design (RIXS)
Energy resolution is fine:
- 100 meV
Energy band is small:
- 500 meV: has to be developed
Alpha-iron anomalous vibrational modes:
- seen even at room temperature;
- increase with temperature;
- anharmonism? magnons?
Measuring DOS is NOT momentum-resolved.
But: it does ideal averaging on momentum, you CANNOT miss something.
Sometimes this makes the difference

## Slide 31
Thank you
for your attention!

## Slide 32: Who did the work:
ESRF:
Rudolf Rüffer
Dimitrios Bessas
Alexey Bosak
Wilson Crichton
Hugo Vitoux
PERTA-III:
Ilya Sergeev
APS:
Yuri Shvyd’ko

## Slide 34
accessible isotopes:
Fe
Sn Sm Eu Dy Sb I Ni Te Xe Ge Os Ru
if required – K Kr Ba Tm

## Slide 36: relevance to an ideal crystalline lattice
57Fe and natural Fe (99.99+%)
foil and single crystal
with and without magnetic field
not from impurities
not from grain boundaries
not from magnetic walls

## Slide 37: not an artefact
elastic peak subtraction
not the multi-phonons
57Fe0.55Ni0.20Cr0.25
no effect in stainless steel
no effect in iron borate
57FeBO3

## Slide 39: Iron at RT with 0.25 meV resolution:
INS data (Neuhaus)
1/2 L [110]
1/2 T1 [110]
1/2 T2 [110]
2/3 L [111]
experiment vs theory
experiment vs convoluted theory
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
Minkievicz = V.G.Minkievicz et al., PR 162, 528 (1967)
- normal trend: upper branches have higher damping;
- not feasible with ~0.6 meV resolution.

## Slide 40: Iron at high temperatures with 0.6 meV resolution:
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
Minkievicz = V.G.Minkievicz et al., PR 162, 528 (1967)

## Slide 41: Iron at 1043 K (TC) with 0.6 meV resolution:
INS data (Neuhaus)
1/2 L [110]
1/2 T1 [110]
1/2 T2 [110]
2/3 L [111]
experiment vs theory
experiment vs convoluted theory
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
- anomaly: lowest branch shows highest damping!
- to check an entire temperature dependence?

## Slide 42: Iron at high temperatures with 0.6 meV resolution:
life-time broadening
decrease of vibrational energy
INS data (Neuhaus)
1/2 L [110]
1/2 T1 [110]
1/2 T2 [110]
2/3 L [111]
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
Yes, anomaly: lowest T2 branch has highest damping.
Furthermore, it’s frequency shows largest decrease!

## Slide 43: the same, but using not theory but LT exp. data for reference:
life-time broadening
decrease of vibrational energy
INS data (Neuhaus)
1/2 L [110]
1/2 T1 [110]
1/2 T2 [110]
2/3 L [111]
Neuhaus = J.Neuhaus et al., PRB 89, 184302 (2014)
The anomaly persists: T2 branch has highest damping
and it’s frequency shows largest decrease.