## Slide 1: Near-field infrared microscopy on carbon nanostructures
Katalin Kamarás
Institute for Solid State Physics and Optics,
Wigner Research Centre for Physics, Budapest
Institute of Technical Physics and Materials Science,
Centre for Energy Research, Budapest

## Slide 2: Resolution in classical microscopy and SNOM (scanning near-field optical microscopy)
- metal coated optical fiber
- drastic decrease in T
E.g.
Transmission
Best:

## Slide 3: s-SNOM: Optical probe
Scattering-type (s-SNOM):
Metallic or metal-coated AFM tip
Resolution
  10-20 nm @
(VIS)
(IR)
Inhomogeneous sample
Classical microscopy
Diffraction limited
N. Ocelic et al., Nature Mater 3, 606–609 (2004)

## Slide 4: What is near field? How do we apply it for detection?
Non-radiating part of an optical field, decays faster than 1/r
Incoming light p-polarized
Directly not detected, still interacts with matter, if it is close enough
Interaction modifies scattered field under metallic probe antenna
Challenge: isolate the part of the field that corresponds to the near field spot
σ scattering coefficient
Notes: The near field can have huge amplitude and huge momentum components
That modifies the scattered propagating field form the metal-coated AFM tip acting as a nano-antenna

## Slide 5: Scattering-type near-field optical microscopy (s-SNOM)
EN – near-field scattering
EB – background scattering
ER – phase modulated reference beam
Light source:
quantum cascade lasers 960 - 1020and 1350 – 1450 cm-1
broadband QCL
synchrotron
DAQ-PC
Ω = 30 kHz, Δz = 30 nm
M = 400 Hz, Δl = 2.2 μm
N. Ocelic, A. Huber, R. Hillenbrand: Appl. Phys. Lett. 89, 101124 (2006)

## Slide 6: Applications of s-SNOM
Nano-identification
  individual molecules: oscillator strength of molecular modes too low
  collective modes (free electrons, phonons)
Quasiparticle mapping
Polariton imaging and interferometry

## Slide 7: Carbon nanotubes
Properties defined by structure
Metallic or semiconducting
Separated fractions available
Different optical properties
H. M. Tóháti, Á . Pekker, B. Á. Pataki, Zs. Szekrényes, K. Kamarás: Eur. Phys. J. B 87, 126–1–6 (2014).

## Slide 8: Analytical model
Based on extended finite dipole model (EFDM)
Substrate-particle-tip system
Approximated with multiple charges generated by the incident E field
Bundles are cylinder-like objects,
approximated with a prolate ellipsoid:
- complex dielectric function – depolarization factor
Simulating the tapping mode: → demodulation→
A. Cvitkovic, Ph.D. thesis, Technische Universität München (2009).
J.Venermo and A. Sihvola, J. Electrostat. 63, 101–117 (2005).

## Slide 9: Analytical calculations
Complex dielectric function of separated
SWCNTs from transmission of self-supporting
films by Kramers-Kronig analysis
Third harmonic phase of d=4 nm bundles
relative to SiO2 substrate

## Slide 10
s-SNOM of metallic and semiconducting nanotubes
Characterizing CNT FETs – substrate SiO2
Distinguish between metallic and semiconducting
Horizontally aligned nanotubes
G. Németh et al., Physica status solidi (b), 253, 2413-2416 (2016)
G. Németh et al., Physica status solidi (b), 254, 1700433 (2017)
Notes: animation

## Slide 11
Carbon nanotube plasmons: single nanotube level
1D plasmons exist in single-walled carbon nanotubes:
1D nature: e-e interaction -> Luttinger-liquid plasmons
Long propagation length – long lifetime
High confinement ratio
High out-of-plane localization of EM field
Zhiwen Shi, Xiaoping Hong, Hans A. Bechtel, Bo Zeng, Michael C. Martin, Kenji Watanabe,
Takashi Taniguchi, Yuen-Ron Shen and Feng Wang, Nature Photon 9, 515–519 (2015)

## Slide 12
SNOM contrast of metallic and semiconducting nanotubes
Where are the plasmons?
  SNR is not enough, sample quality
Literature lacks the full midIR contrast spectrum
@ neaspec HQ
??? SiO2 phonons ???
It should be a peak, not a dip
There is only native oxide
Strong coupling?

## Slide 13
Interaction of plasmons with substrate phonons (Si, hBN)
Clear plasmon interference fringes
Silica and hBN phonons:
  Silica:
  hBN:

## Slide 14
Wide-range measurement
Sequential spectral imaging 920-1720 cm-1 with 20 cm-1 steps
Plasmon wavelength changes
Fringe contrast dramatically changes
Nanotube becomes invisible in the respective Reststrahlen bands
Strong field confinement
Strong coupling
Enhanced sensitivity
(molecular detection)

## Slide 15: C60@BNNT
Growth of Carbon Nanotubes inside Boron Nitride Nanotubes by Coalescence of Fullerenes: Toward the World’s Smallest Coaxial Cable
Kate E. Walker, Graham A. Rance,* Áron Pekker, Hajnalka M. Tóháti, Michael W. Fay, Rhys W. Lodge, Craig T. Stoppiello, Katalin Kamarás, and Andrei N. Khlobystov*
Small Methods 1, 1700184 (2017)

## Slide 16: C60 in BNNT – interaction with phonon-polaritons
D. Datz, G. Németh, K.E. Walker et al. ACS Appl. Nano Mater. 4, 4335 (2021)
Detection threshold:
~ 160 molecules
Coupling of
phonon-polaritons to
molecular vibrations

## Slide 17
Photo-oligomerization
Far-field absorption
n = 1
n = 2
n = 3
n = 3
Wavenumber [cm-1]
D. Datz, G. Németh, K.E. Walker et al. ACS Appl. Nano Mater. 4, 4335 (2021)

## Slide 18: Tip-enhanced Raman Spectroscopy (TERS)
C.D. Tschannen, T.L. Vasconcelos, L. Novotny: J. Chem. Phys. 156, 044203 (2022)

## Slide 19
Graphene nanoribbons in carbon nanotubes
1
2
3
4
5
6
dCH
dCH
dGNR
dvdW
dvdW
Nanoribbon
Nanotube

## Slide 20
NT RBM
Topography
NR RBLM
NT+NR G mode
A. Cadena, B. Botka, Á. Pekker, C.D. Tschannen, C. Lombardo, L. Novotny, A.N. Khlobystov, K. Kamarás: J. Phys. Chem. Lett. 13, 9752 (2022)
TERS on NR@NT
(Cla Duri Tschannen,
Lukas Novotny,
ETH Zürich)

## Slide 21
Dániel Datz
Gergely Németh
Áron Pekker
Erzsébet Dodony, Zsolt Fogarassy, Béla PéczResearch Institute for Technical Physics and Materials Science
Cla Duri Tschannen, Chiara Lombardo, Lukas Novotny
ETH Zürich
Adrian Cernescu
Neaspec – Attocube GmbH, Munich
Keigo Otsuka, Taiki Inoue, Shigeo Maruyama
The University of Tokyo
Kate Walker, Graham A. Rance, Andrei N. Khlobystov
University of Nottingham
Hidetsugu Shiozawa
University of Vienna
Collaborators
Bea Botka
Ana Cadena
Ferenc Borondics

## Slide 22: Funding
OTKA FK 125063, K 143153 – operating costs
SZFKI -> Wigner
NeaSNOM original investment
2012, funded by MTA
Major upgrade
2019, funded by ELKH
MTA -> ELKH
ELKH -> HUN-REN
????????