## Slide 1: Ultrafast electron processes in solids
Dombi Péter

## Slide 2: 1. Ultrafast electron processes in plasmonic systems
Plasmonic hot electron generation and decay
(1-1000 fs)
Photoemission (even in attoseconds if tunneling)

## Slide 3
approach for measuring field enhancement
fs near-field stimulates photoemission
spectra of photoelectrons can be measured
photoelectrons rescattered at the surface have the highest kinetic energy
4. Qmax = 10,007 e2λ2Eloc2 / (16 2mc2)
5. rescattering takes place in nanometric volumes
Near field maximum can be measured with photoelectrons
P. Rácz… P. Dombi, Nano Lett. 17, 1181 (2017)
Notes: …Well-known it atomic physics as ATI, however, its counterpart with the photoemission from solids has not been exploited so far for any practical application

## Slide 4
36.1 vs. 31.7
51.2 vs.50.5
P. Rácz…P. Dombi, Nano Lett. 17, 1181 (2017)
← experiment vs.
simulation
Validation

## Slide 5: Nonadiabatic nanooptical tunneling of photoelectrons
B. Lovász…P. Dombi,
Nano Lett. 22, 2303 (2022)

## Slide 6: Ultrafast electron processes in plasmonic systems
Plasmonic hot electron generation and decay
(1-1000 fs)
Photoemission (even in attoseconds if tunneling)

## Slide 7
Hot electrons and their plasmon mediated excitation
Hot electrons: electrons with energy levels differing significantly from the Fermi-Dirac distribution at the given temperature
N.Nanotechnology 10, 25 (2015)
Adv.OpticalMater. 2020, 8, 1901166

## Slide 8
Typical timescales of electron excitation
photon absorption drives the electron distribution out of equilibrium
electron-electron scattering: high temperature Fermi–Dirac distribution
electron–phonon interactions: reduction of this electron temperature on a picosecond time scale
Processes following SPP excitation // each process has its own f(E):

## Slide 9
What can e2 tell us about the excitation/decay of SPPs?
where
ε2,intra is the contribution from intraband transitions
D is the energy distribution of the joint density of states
f(E) is the electron energy distribution
→ by measuring ε2, we can extract information on f(E), therefore on hot electrons!
Budai, Pápa, Petrik & Dombi, Nature Comm. 13, 6695 (2022)

## Slide 10
A very sensitive way to measure ε2 is ellipsometry
Hot electron measurement concept:
to generate difference data with and without plasmon excitation

## Slide 11
Ellipsometry model to reproduce measured data
Au with hot electrons: ε2,top
Au without hot electrons: ε2,bottom
substrate: ε2,substrate
variable thickness in model

## Slide 12
What is the thickness of the upper hot electron layer?
Changes with laser power between 4.5-6.5 nm
CW excitation – retrieving e2
The measured difference curves are perfectly reproduced
Budai, Pápa, Petrik & Dombi, Nature Comm. 13, 6695 (2022)

## Slide 13
How much do the dielectric function of the upper and the lower layer differ?
0.2 eV shift of interband bandedge due to hot electrons (2.5 eV vs. 2.3 eV)
CW excitation – retrieving e2

## Slide 14
Conclusion
4.5-6.5 nm
50 nm
Budai, Pápa, Petrik & Dombi, Nature Comm. 13, 6695 (2022)
…performed with novel ellipsometric probing

## Slide 15
Compare ultrafast intraband (800 nm pump) and interband (480 nm pump) excitations of gold at the nanoscale
New pump-probe method developed @Wigner: plasmon wavepacket as a probe for nonthermal electrons
Time-resolved pump-probe experiment

## Slide 16
Ultrafast dynamics after photoexcitation

## Slide 17
We measured a 2-component ultrafast decay of hot electron populations

## Slide 18
THREE-TEMPERATURE-MODEL (3tm) to explain 2-comp. Decay
Pump affects optical properties of gold layer -> three-temperature model (3TM)
absorption coefficient (a) and reflection (R: 35% vs. 97%) different for 480 nm and 800 nm
Largest modulation ~ when energy stored in nonthermal electrons (N) is maximal in 3TM
Three-temeprature model to reproduce measurement

## Slide 19
Three-temeprature model results
Lovász et al., submitted (2023)

## Slide 20: Collaboration with TU Graz (Martin Schultze): ultrahigh resolution plasmon nanoscopy

## Slide 21: Carrier-envelope phase detector based on transient metallization of dielectrics
V. Hanus…P. Dombi, Optica, 8, 570 (2021)
V. Hanus…P. Dombi, Nature Commun., 14, 5068 (2023)

## Slide 22: 3D phase scanning and scuplting
V. Hanus…P. Dombi, Optica, 8, 570 (2021)
V. Hanus…P. Dombi, Nature Commun., 14, 5068 (2023)

## Slide 23
Conclusions
Nonadiabatic tunneling from nanoparticles
(Lovász, Nano Lett. 2022)
Ultrasensitive hot electron detection
(Budai et al. Nature Comm. 2022)
Plasmon probing of hot electron decay
(Lovász et al., 2023)
Optical chip for phase scanning and sculpting of laser beams
(Hanus et al., Nature Comm. 2023)

## Slide 24
Open positions:
dombi.peter@wigner.hu
www.femtolab.hu
Thank you - lab members
P. Rácz, P. Sándor, V. Hanus, K. Vereb, Z. Pápa, V. Csajbók,
B. Fehér, B. Lovász, B. Bánhegyi, G. Ligeti, G. Z. Kiss

## Slide 26
N.Nanotechnology 10, 25 (2015)
After the excitation of SPP their energy is transfered to the electron subsystem and afterwards to the lattice
1st step of this process: hot electron generation
Surface plasmon polaritons (SPP) - collective charge-density oscillations and the coupled EM wave
~100 nm

## Slide 27
Understanding e2
Why do we observe hot electrons with energies only up to 0,4 eV?
Based on the 1.55 eV excitation photon energy one would expect higher photon energies
e--e-scattering energy dependent => only less energetic electrons can be observed
generation of SPP
CW excitation:
all sc. process are present and
the electron excitation is continued => a region with different e- distribution
energy transferred to the electron subsystem
energy distributed via e- - e- and e- - phonon scattering

## Slide 28
What can e2 tell us about the excitation/decay of SPPs?
photon absorption drives the electron distribution out of equilibrium
electron-electron scattering: high temperature Fermi–Dirac distribution
electron–phonon interactions: reduction of this electronic temperature on a picosecond time scale
The different time-delays can be attributed to different process following SPP excitation
Each process have its own f(E):
t ≈ 600 fs
electron temperature increases due to e--e- interactions
t≈100 fs
photon absorption
t<0
before the excitation
few-ps
electrons interact with phonons
ps range
lattice thermalization
Dubi and Sivan, Light: Sci. & App. 8, 89, 2019.

## Slide 29
Interband and intraband excitation pathways with 480 nm and 800 nm pumps
Govorov et al. J. Phys. Chem. C 2013 117, 32
Notes: So here you can see the band structure of gold, and there are pathway for 800 nm intraband exitations, and 480 nm interband exitations