## Slide 1
HIGH FIELD NANOPLASMONICS FOR NUCLEAR FUSION
NORBERT KROO
WIGNER RESEARCH CENTER OF PHYSICS
(on behalf of the NAPLIFE project)
PP2024: 11.06.2024

## Slide 2
1.Material in extreme conditions
I = 1016 W cm-2
Tunnelling
1014 - 1015 W cm-2
free
atom
+
Slope: 4.3+/-0.4
(perturbation)
Slope: 0.89+/-0.03
(tunnelling)
4.10¹⁰ W/cm²

## Slide 3
2.The optical near field

## Slide 4
Ti:Sa laser: ʎ=800nm (~1.55eV) ; t(SPP)~30fs
SPP
LSPP
PLASMONICS AND HIGH FIELDS APPLICATIONS
Special type of the optical near field
ω(eV)

## Slide 5
1.SURFACE PLASMON POLARITONS (SPP)

## Slide 6
A fény hullámhossznál sokkal kisebb méretű lyukakon (réseken) is áthalad
AZ ENERGIA ZÖME A FELÜLETRE KONCENTRÁLÓDIK: ÓRIÁSI TÉR ERŐSÍTÉS
VÁKUUM
FÉM
NAGYSZÁMÚ POTENCIÁLIS ALKALMAZÁS.

## Slide 7
2.LOCALIZED PLASMONS (LSPP) UP TO 10²⁰ W/cm²)
(The basic difference between SPP-s and LSPP-s)
LSPP: -NO PENETRATION INTO THE PLASMONIC MATERIAL (e.g. metal)
- SMALLER PENETRATION INTO THE DIELECTRIC /VACUUM
-NO DISPERSION, RESONANCE DEPENDS ON SIZE, SHAPE, MATERIAL
-BROADER RESONANCE

## Slide 8: PLASMON RESONANCE OF NANOPARTICLES SHAPE AND- ÉS SIZE DEPENDENT!
Sphere
Bulk
Nanoshell:
a
b
Üreg
Nanoshell plasmon resonance depends on the x ratio .
Surface

## Slide 9
Spectral tuning range
nanoshell plasmon rezonance
0
2
4
6
8
10
1
10
100
1000
Wavelength (microns)
Core/Shell Ratio r1/(r2-r1)
1.24 electron volts 0.124
10,000 cm-1 1,000
300 THz 30
r2
r1
e2
e1
e3

## Slide 10
Nanorod:Transverse and longitudinal modes!
T
L

## Slide 11
Krystina Kolwas: Materials 2023, 16,1801, pp1-15

## Slide 12
-HOT SPOT
-SCREENING
-PONDEROMOTORIC
ACCELERATION
-CORRELATED MOTION

## Slide 13
AND UP TO ~10²⁰ W/cm²

## Slide 14
SIMULATION OF PROTON AND ELECTRON ENERGIES AT A SINGLE NANOROD

## Slide 15
Some potential new energy technologies
(involving nanotechnologies)
P3HT Cell efficiency = 6%
SPESC (P3HT) efficiency = 17.5%
Toward our proposal

## Slide 16
NIF (LÉZER INDUKÁLT FÚZIÓ)
192 lézer, 400MJ, a targeten 2MJ. A generált nukleáris energia 3MJ. Egy target kapszula ára ~10⁵USD. A lézerimpulzus hossza : 10-50ns , 1 imp/nap. A berendezés ára: sokmilliárd USD.
10⁵USD
Target tartó

## Slide 17
FEMTOSECOND LASER PULSES;
HIGH REPETITION FREQUENCY;
LIGHT SPEED: NO TIME FOR INSTABILITIES; ONLY TWO BEAMS; TIMELIKE VOLUME IGNITION
d ~ n.10μ
NANOPARTICLES IN THE FUSION MATERIAL
NANOSHELL
(nx10nm)
NANOROD (~85x25nm)
:
n.10μ
NANOPLASMONICS AND ENERGY CONCENTRATION
Λ=800nm

## Slide 18
Ti:Sa laser

## Slide 19
LIGHT-MATTER INTERACTION:
PLASMA-MIRROR REFLECTIVITY
(how can light enter into matter? )
Ch.Ziener at al : J.Appl.Phys. 93,768 (2013)
MY PAST EXPERIENCE
PRESENT AND FUTURE

## Slide 20
Minta: polimer (UDMA+ TEGDMA) Au2 (0.18m/m%) rezonáns nanorúd
és Au0 (nanorudak nélkül)

## Slide 21
d = 160μ

## Slide 23
Chart: Longitudinal position [mm]
| 3.6 | 3.6 | 3.4 | 3.2 | 3 | 2.8 | 2.6 | 2.4 | 2.2000000000000002 | 2 | 1.8 | 1.6 | 1.4 | 1.2 | 1 | 0.6 | 0.4 | 0.2 | 0 | 0 | -0.2 | -0.4 | -0.6 | -0.8 | -1 | -1.2 | -1.4 | -1.4 | -1.6
Volume Au2 - 10 mJ | 95250.9997 | 96412.5951 | 84604.3971 | 75419.9867 | 101118.1905 | 85074.2044 | 84343.0544 | 72965.3383 | 52681.584 | 56078.2645 | 49107.967 | 44054.0456 | 55422.8732 | 107902.4535 | 81869.3538 | 40089.1545 | 30865.173 | 32390.752 | 41080.8234 | 40356.2222 | 50275.0579 | 56164.0722 | 67908.6305 | 75215.5697 | 85022.5776 | 99452.937 | 105115.5811 | 105135.5948 | 121388.9403
Volume Au2 - 25 mJ | 171796.1935 | 77927.0397 | 77317.6986 | 322204.1442 | 524509.451 | 367102.8715 | 381845.7952 | 163521.643 | 108193.0954 | 90780.4479 | 84447.4949 | 77988.3685 | 85079.5249 | 92261.1921 | 102338.1659 | 89308.4281 | 94785.608 | 72368.2911 | 85196.9421 | 93173.6331 | 125389.8206 | 473151.6989 | 458566.0215 | 343329.69 | 239761.3744 | 129269.2734 | 118171.6763 | 142357.8027 | 111276.5142 | 112844.0347 | 161534.9375
2,5.10¹⁷W/cm²
2.10¹⁷W/cm²
1,2.10¹⁷W/cm²
0,5.10¹⁷W/cm²
Chart: Longitudinal position [mm]
| 0 | 0 | 0.2 | 0.6 | 0.6 | 0.8 | 0.6 | 0.4 | 0.2 | 0 | -0.2 | -0.2 | -0.4 | -0.6 | -0.8 | -0.6 | -0.4 | -0.2 | 0 | 0.2 | 0.4 | 0.6 | 0.6 | 0.8 | 1 | 1.2 | 1.4 | 1.4 | 1.6 | 1.8 | 2.6
Volume - Au2 - 25 mJ | 171796.1935 | 77927.0397 | 77317.6986 | 322204.1442 | 524509.451 | 367102.8715 | 381845.7952 | 163521.643 | 108193.0954 | 90780.4479 | 84447.4949 | 77988.3685 | 85079.5249 | 92261.1921 | 102338.1659 | 89308.4281 | 94785.608 | 72368.2911 | 85196.9421 | 93173.6331 | 125389.8206 | 473151.6989 | 458566.0215 | 343329.69 | 239761.3744 | 129269.2734 | 118171.6763 | 142357.8027 | 111276.5142 | 112844.0347 | 161534.9375
Volume - Au0 - 27,7 mJ | 160946.9652 | 142535.4683 | 128882.9043 | 114670.3694 | 92810.559 | 76026.8821 | 69164.4553 | 70659.7141 | 66100.6033 | 57342.2355 | 49468.179 | 43929.63 | 46265.5601 | 66359.7642 | 112720.194 | 142992.3673 | 74496.5466 | 86969.5341 | 92720.0729 | 105941.9971 | 115066.9048 | 134806.2899 | 157088.4402 | 163777.4392 | 178881.1504 | 191782.9598
HIGH FIELD PLASMONICS WORKS!
CRATER VOLUMES
0,46.10¹⁷W/cm²

## Slide 24
1,2.10¹⁷ W/cm²
Volume ~3,5 V₀

## Slide 25
25mJ
27.5mJ
Crater volume: ~ Elaser imp.
Volume increase: ~ Ilaser imp

## Slide 26
Au0 12.3fs
Au2 12.3fs
Au0 42fs
Au2 43fs
CRATER VOLUME IMAGES TAKEN AT WIGNER AND ELI (25mJ pulse energy)
WIGNER
Au0 42fs
ELI
ELI
ELI
ELI
WIGNER
Au2 42fs
ELI
ELI
Au0 12.3fs
Au0 43fs

## Slide 27
Ilaser > 10¹⁶ W/cm²
2.Diagnozis :Raman scattering from the crater surface
a
b
arXiv2210.00619(2022),submitted to Advanced Optical Materials
Au0
Au1
Au2

## Slide 28
2D+H The total number of H atoms before the transmutation process
Number of D atoms in the case of 25mJ laser pulses : ~1.76x10¹⁵
3.SOME RESULTS OF THE Hᵅ AND Dᵅ SPECTRAL LINES
Deuterated (30%) sample
D
H
D
H

## Slide 29
Au2
Au0

## Slide 30
798 Au2 12.3fs
102 Au0 12.3fs
4
1
12
12
6

## Slide 31
HIGH INTENSITY PLASMONICS WORKS

## Slide 32
With boron Au2 12.3fs
With boron Au0 12.3fs
6
4
3
1

## Slide 34
H?
D?
LET
LET (kev/micron)
DIAMETER (micron)

## Slide 35
DIAMETER (micron)
α

## Slide 36
LET (KeV/micron)
α

## Slide 37
CONCLUSIONS
1.Table-top lasers have been found to indicate the significant role of
high field nanoplasmonics in potential nuclear fusion processes.
2.Above ~ 10¹⁷W/cm² laser intensity the formation of reflective
plasma mirror is negligible, light penetrates into the sample.
3.Plasmonics works also at high laser intensities.
-Significant energy production has been detected, indicated by
the increase of the crater volume and Thomson parabola results
of BN seeded samples
-The source of this excess energy could be partly the deuterium
production, detected by optical spectroscopical methods.
-The particle energy of ions in the plume is always higher for
samples with resonant plasmonic nanoparticles than for those
without them.
-The Thomson parabola spectrometer spectra indicate also this
influence of the LSPP resonance effect on the basic processes.
4.Nuclear processes have also been indicated, but here further, more
convincing studies are needed.

## Slide 38
THANKS FOR YOUR ATTENTION!

## Slide 39: When the winds of changes are blowing some build shelters, but some others build wind turbines