## Slide 1: Materials challenges in quantum sensing with diamond nitrogen-vacancy center
Adam Gali
Recent advances in quantum computing and technology (ReAQCT)
June 19-20, 2024, Bosch Budapest Innovation Campus, Hungary
HUN-REN Wigner Research Centre for Physics, Budapest, Hungary
Budapest University of Technology and Economics, Budapest, Hungary
ReAQCT 2024

## Slide 2
Introduction
James N. Eckstein and Jeremy Levy, MRS Bulletin 38, 783, (October 2013)
Development of materials to single atom limit
Development of spectroscopy to single photon limit

## Slide 3
Introduction
single photon emitter, single spin
J. Meijer et al., APL 87 261909 (2005)
J.R. Rabeau et al., APL 88 023113 (2006)
implantion of N ions: create vacancies
annealing at T>700 °C: formation of NVs
acid cleaning of the damaged surface

## Slide 4
Introduction
Optically Detected Magnetic Resonance – ODMR
Maze et al., New Journal of Physics, 14, 103041 (2012)
Long coherence time at room temperature

## Slide 5
NV center in diamond: one spin to sense them all
Electric field sensing
Strain and pressure sensing
Thermometry
Force sensing and gravitometry
Magnetic field sensing
measure temperature at the nanoscale: single (biological) molecule
Revolutionize chemistry, biology and medical diagnostics
gyroscopes on chip operating at harsh environments
Revolutionize (self-driven) automotive industry, navigation systems
portable gravitometry
Revolutionize geographical science and astronomy

## Slide 6
NV center: magnetometer for solid state physics
Casola et al., Nature Reviews Materials, 3, 1 (2018)

## Slide 7: Shallow nitrogen-vacancy centers in diamond
nearby vacancies and divacancies are formed
Nat. Comms. 8, 1549 (2017)
Nano Letters 14, 4772 (2014)
oxygen termination for nearly positive electron affinity
Nat. Elec. 1, 502 (2018)
band bending (negative species at the surface)

## Slide 8: Charge transition levels of defects in diamond
Phys. Rev. B 89, 075203 (2014)
green illumination ionizes neutral single vacancies and divacancies with creating holes
NV− has a giant hole capture cross section [Nat. Elec. 4, 717 (2021)]
V2
V

## Slide 9: Modeling of diamond surface and band bending
A. Gali, Nanophotonics, 8, 1907-1943 (2019)
A. Gali, Nanophotonics, 12, 359-397 (2023)
Methodology: ab initio DFT and beyond
Ambient condition: absorbed water on top of diamond surface
ab initio molecular dynamics to cover diamond with water
carboxyl groups (COOH) represent acceptor defects at the surface
Electron affinities (vacuum level shifts and work functions) can be determined

## Slide 10: Results: low pressure is the problem
Large band bending causes the instability of deep defects’ charge state under illumination (V2− → V20)
V20 emmits a hole (V20 → V2− + h+), which is captured by the NV (NV− + h+→ NV0)
Water, reducing the band bending, extends the stability region towards the surface
The effect originates from the low pressure applied in the cooling process rather than low temperature

## Slide 11: Results: experimental verification
single NV− ODMR signal disappears at room temperature after applying low pressure

## Slide 12: Results: experimental verification
ODMR signal disappears at ~4 K, so that the antibunching feature
PL implies that NV− gets ionized to NV0
Spraying water (1-2 nm layer) leads to revival of the ODMR signal of single shallow NV centers
with A. Singha @ MPI in Stuttgart, Nano Letters, 23, 2563 (2023)

## Slide 13: Results: electrolyte (NaCl) solution
−
+
interfacial dipole moment is developed
water at room temperature electrolyte at room temperature
COO−H+
COO−Na+
experiments with D. Bucher @ TU München, ACS Nano, 17, 10474 (2023)

## Slide 14: Results: electrolyte (NaCl) solution
experiments with D. Bucher @ TU München, ACS Nano, 17, 10474 (2023)
Marcus-theory for calculating the electron (charge and spin) hopping
slow for P1 center, 0.1 GHz for vacancies at a distance of 3 nm in contact with water
It slows down with an order of magnitude caused by interfacial dipole field in contact with electrolyte
T1 times of NV and the dark spins increase

## Slide 15
Observed single photon sources and quantum bits
A. Gali et al., Appalied Physics Reviews, 7, 031308 (2020)
exp. confirmed qubits
Room temperature qubits
Diamond NV
Science 276, 2012 (1997)
SiC VSi-center (low contrast)
Nat. Mat. 14, 164 (2015)
SiC divacancy (high contrast)
Nature 479, 84 (2011)
Nat. Comm. 4, 1819 (2014)
Nat. Sci. Rev. 9, nwab122 (2022)
Quantum guidelines for solid-state defect spins, Nature Reviews Materials 6, 906 (2021)

## Slide 16: Quantum Technology Summer in Budapest
154 attendees, 28 countries from 5 continents

## Slide 17: Summary
charge state of shallow vacancies should be controled
absence of water is the problem for the oxygen-terminated diamond NV quantum sensor in cryogenic temperature operation
this can be resolved by water dosing
biomedical sensor applications are viable (e.g., blood serum)
Acknowledgement
Horizon Europe
Nano Letters, 23, 2563 (2023)
ACS Nano, 17, 10474 (2023)
Anton Pershin

## Slide 18: Magneto-optical spectroscopy research group

## Slide 19: Supplementary Materials

## Slide 20
KS DFT APES
Derived APES
electron-phonon Hamiltonian in (A1 + E) x E el-ph space
Damped pseudo Jahn-Teller effect
HUN-REN Wigner Research Centre for Physics, Adam Gali

## Slide 21
Damped dynamic Jahn-Teller effect combined with pseudo JT effect
HUN-REN Wigner Research Centre for Physics, Adam Gali

## Slide 22
Damped dynamic Jahn-Teller effect combined with pseudo JT effect
HUN-REN Wigner Research Centre for Physics, Adam Gali

## Slide 23: NV center: sketch of typical ODMR setup
optical path
Confocal microscope
Microwave
Photodetectors
Photoexcitation
optical readout of single spin
Science 276, 2012 (1997)

## Slide 24
Important properties
E ±1
A1 0
D: zero-field splitting
(c)
T2≈1 ms @ RT
30% readout
contrast
Magnetic field,
electric field,
strain field and temperature dependence
e spin – e (n) spin interaction

## Slide 25
Methodology
Born-Oppenheimer approximation (adiabatic potential energy surface)
HSE06 hybrid Density Functional Theory functional (almost no band gap-error)
electronic structure and spin-density distribution
constrained occupation DFT for excited state calculation
[Gali et al., Physical Review Letters 103 186404 (2009)]
512-atom supercell with G-point sampling of BZ

## Slide 26
Typical characterization: thermodynamics
(0)
(½)
(1)
(½)

## Slide 27
Developments and implementations
impact ionization and Auger-Meitner rates [PRL (2013); PRB 87 155402 (2013)]
hyperfine coupling [PRB 88 075202 (2013)]
electron spin – electron spin coupling (zero-field splitting) [JP:CM 26 015305 (2014); PRB 90 235205 (2014)]
treatment of highly localized d-electrons [PRB(2013); 90 035146 (2014)]
interaction of quantum wells (stacking faults) and point defects [Nanoscale 6 10027 (2014); Nature Communications 6 7783 (2015)]
comprehensive theory of optical nuclear spin polarization [PRB (2020)]
modeling of complex surfaces and quantum confinement effects [Nature Nanotechn. 9 54 (2014); Nano Letters 14 4772 (2014); JP:CM 26 143202 (2014)]
CI+cRPA method for excited state calculation [npj Quantum Materials 3, 31 (2018)]
intersystem crossing (ISC) rates [PRB 96, 081115(R) (2017); 98, 085207 (2018)]
Spin-orbit coupling and ISC: should go beyond Born-Oppenheimer approximation

## Slide 28
General considerations: why Jahn-Teller systems
high spin ground state
degenerate orbitals
degenerate orbital
Jahn-Teller instability

## Slide 29
General considerations: spin-orbit coupling (SOC)
orbitally degenerate state with spin
non-zero spin-orbit coupling
like a p electron
mL=±1
lz Lz Sz
mS=±1/2
mJ=±1/2
mJ=±3/2
lz

## Slide 30
Jahn-Teller systems in defect qubits
NV center
SiV center
Thiering & Gali, PRB Rapid 96, 081115
Thiering & Gali, PRX 8, 021063

## Slide 31
Jahn-Teller systems in defect qubits
3E excited state at a closer look
lz
lz
{A1, A2}
E (0)
E (±1)

## Slide 32: Understanding ISC and optical spinpolarization
Group Theory predicts no effective intersystem crossing (ISC)
✘
3E excited state: Exe dynamic Jahn-Teller system
pseudo Jahn-Teller interaction: (A1 + E) x e system

## Slide 33: Understanding the effective spin-orbit coupling
3E excited state: Exe dynamic Jahn-Teller system*
n, m quanta of eX, eY phonons
I. Bersuker, The Jahn-Teller effect (Cambridge University Press, 2006).
Frank S. Ham, Phys. Rev. 138, A1727 (1965)
lzeff = p lz
Ham reduction factor p
*K.-M. C. Fu et al., PRL 103 256404 (2009)
T. A. Abtew et al., PRL 107 146403 (2011)

## Slide 34: Understanding ISC and optical spinpolarization
3E excited state: Exe dynamic Jahn-Teller system
p = 0.307
lZ(eff) = p lZ =
0.307 × 15.78 GHz =
4.86 GHz
lZ(exp) ≈ 5.0 GHz

## Slide 35: Understanding ISC and optical spinpolarization
3E excited state: Exe dynamic Jahn-Teller system
n, m quanta of eX, eY phonons
vibronic wavefunctions
≈ 0.5
Thiering & Gali, PRB Rapid 96, 081115

## Slide 36: ISC at lower branch: spin-orbit coupling with singlets
lz
l

## Slide 37: ISC at lower branch: spin-orbit coupling with singlets
Electron-electron interaction
brings (damped) dynamic Jahn-Teller interaction

## Slide 38: ISC at lower branch: spin-orbit coupling with singlets
Electron – phonon coupling:
damped pseudo Jahn-Teller interaction
Electron-electron interaction:
brings (damped) dynamic Jahn-Teller interaction
Quantum guidelines for solid-state defect spins, Nature Reviews Materials 6, 906 (2021)

## Slide 39: Understanding ISC and optical spinpolarization
Damped pseudo Jahn-Teller interaction: (A1 + E) x e system

## Slide 40: Understanding ISC and optical spinpolarization
Damped pseudo Jahn-Teller interaction: (A1 + E) x e system
✓
broad feature in phonon sideband
forbidden phonon peak in between
✓

## Slide 41: Understanding ISC and optical spinpolarization
Damped pseudo Jahn-Teller interaction: (A1 + E) x e system
≈ 6
temperature dependence
✓
NJP 13, 025013 (2011)
Thiering & Gali, PRB 98, 085207

## Slide 42
NV center in diamond: T1 time with temperature
RT operation: large triplet-singlet gap and large phonon energies w.r.t. zero-field-splitting energy
PRL 130, 256903 (2023)
double exponential (Orbach-like) decay with 65-meV and 165-meV effective modes activated by temperature
T1 time ≈ 1 ms at room temperature
quasi-local vibration modes