## Slide 1: Exchange-driven hole spin qubit in Germanium
Jaime Saez-Mollejo
ReAQCT 2024, Budapest
June 19th 2024

## Slide 2: Introduction to spin qubits in Ge
  Why Ge?
  Strong spin-orbit interaction  Fast electrical driving
  Low hyperfine interaction  Increase of coherence time
  Compatible with superconducting technologies 
Hendrickx et al. Nature (2020)
Watzinger et al. Nature comm. (2018)
Wang et al. arxiv (2024)
Our goal: understanding the Physics of holes
Germanium has become really interesting platform for spin qubit experiments
A gate tunable transmon qubit in planar Ge (arXiv:2403.16774v1)

## Slide 3: Our design
80 nm
Microwave source
Reflectometry circuit
Ohmic contact
Ge
18 nm
20 nm
Confinement
Occupation
Holes accumulated at V=0
Cross section
Top view
Microwave source
Material: Isella group
Notes: 2D heterostructure grown by our collaborators in Como
Not deeply buried
Microwaves generate and effective magnetic field via SOI interaction
To read the qubit we measure a reflected RF signal in the sensor

## Slide 4: Readout: a simple picture of Pauli spin blockade
‘1,1’
‘0,2’
‘1,2’
‘0,1’
Signal low
Signal high
A
C
B
Spin-to-charge conversion!
Ono et al. Science (2002)
Johnson et al. PRB (2005)
+
Driving
B
C
A
Sensitive to charge occupation

## Slide 5: Find the qubit line: Magnetic spectroscopy
Nadj-Perge et al. PRL (2012)
Ono et al. PRL (2018)
,
,
Spin transition of 2-spin states. Why?
, ,
Spin transitions of single spin states
Nadj-Perge et al. PRL (2012)
Similar spectroscopy J-dominated
In-plane magnetic field

## Slide 6: Magnetic spectroscopy
Fixed 
Fixed B=0
B
C
A
‘1,1’
‘0,2’



Tunability of exchange interaction, J, with detuning
S
Uncommon feature
 transition is a double spin flip  Typical driving results in single spin flips

## Slide 7: ST qubit with orthogonal rotation axis
By fitting the magnetic spectroscopy
Extracting all the parameters we verify we are in the ST basis
Jirovec et al. Nature Mat. (2021)
ST qubits NOT microwave driven
Here we show a microwave driven ST qubit with orthogonal axis
Previous work in the group:
Rotation axis is not orthogonal
Imposing constraints to the operation
MW driving provides orthogonal axis

## Slide 8: Can they be coherently driven?



Why can we drive them?
Why do they have different Rabi frequencies?

## Slide 9: Driving mechanism
Froning et al. Nature Nano (2021)
Studying the Rabi frequency vs B and  we obtain information about the driving mechanism
Electric Dipole Spin Resonance or g-tensor Magnetic Resonance
J and follow the same trend with detuning

## Slide 10: Driving mechanism
Microwave source
AC electric field applied on BR is coupled to the detuning of the DQD
Modulation of exchange
As a result:
: Lever arm on the quantum dot
: Amplitude of microwave burst
H=
Off-diagonal terms which drive the system

## Slide 11: Driving mechanism: exchange modulation
Froning et al. Nature Nano (2021)
Studying the Rabi frequency vs B and  we obtain information about the driving mechanism
Electric Dipole Spin Resonance or g-tensor Magnetic Resonance
J and follow the same trend with detuning

## Slide 12: Driving mechanism: exchange modulation
Studying the Rabi frequency vs B and  we obtain information about the driving mechanism
J and follow the same trend with detuning
Theory exchange modulation driving (solid lines)
Froning et al. Nature Nano (2021)
Electric Dipole Spin Resonance or g-tensor Magnetic Resonance

## Slide 13: What about out-of-plane?



Open questions:
and transitions are not coherent?
Why we don’t observe EDSR or g-TMR driving?
Rabi frequencies also compatible with exchange modulation
Jirovec et al. Nature Mat. (2021)
This qubit was out-of-plane
Magnetic spectroscopy
Initial state is a S

## Slide 14: Summary
Thank you for your attention!
S. Bosco
M. Rimbach-Russ
D. Jirovec
G. Isella
D. Chrastina
A. Ballabio



Take home messages
Transitions driven are two-spin states
Exchange modulation causes the driving
ST qubit with orthogonal axis
G. Katsaros
Y. Schell

## Slide 15: How to drive a spin qubit: oscillating magnetic field
Koppens et al. Nature (2006)
Novak et al Science (2007)
Strip line
Micromagnet
Spin orbit mediated
Pioro-Ladrière et al. Nature Physics (2008)
No strip line or micromagnet needed!
Notes: https://www.nature.com/articles/nature05065
https://www.science.org/doi/epdf/10.1126/science.1148092

## Slide 16: Two-photon process
Single photon process
Two-photon process