## Slide 1: AIME 2025 Designing (Chasing) topologial qubit with HPC
Balázs Újfalussy
HUN-REN Wigner Research Center for Physics, Budapest
Notes: Fundametals of SKKR-Bogoliubov-deGennes theory

## Slide 2
Quantum computers
    noisy intermediate-scale quantum computers: operations limited by coherence time and gate fidelity
(1)
(2)

## Slide 3
Potential qubits
James N. Eckstein and Jeremy Levy, MRS Bulletin 38, 783, (October 2013)
Topological protection solves
the decoherence problem
Small
Scalable
Majorana 1: chip with 8 topological qubit
Nature 638, 872 (2025)
https://news.microsoft.com/azure-quantum/

## Slide 4
Majorana Fermions
Fermionic basis:
Majorana basis:
Ettore Majorana, 1937, Nuovo Cimento 5, 171
Neutrinoless double beta decay (0νββ) not yet detected
it’s own antiparticle
Notes: Dirac fermion is described by a (non-Hermitian) Dirac operator ci that satisfies fermionic anticommutation relations,

## Slide 5
Kitaev chain and Majorana Zero Modes
Kitaev, A., 2001, Phys. Usp. 44, 131.
zero-energy MZM at the end of the chain
Chemical potential
N.N. hopping
Spinless p-wave pairing
In Majorana basis:

## Slide 6
Topological quantum computation with MZM
J. Alicea et al., Nat. Phys. 7, 412 (2011)
    Majorana bound state described by and Majorana operators
    stable against local decoherence, topologically protected operations when exchanging them
    require p-wave superconductivity or s-wave pairing, magnetism and spin–orbit coupling

## Slide 7: STM/STS experiments on magnetic chains
Fe chains on Re(0001)
H. Kim et al., Sci. Adv. 4 eaar525111 (2018)
Mn chains on Nb(110)
L. Schneider et al. Nat. Nanotechnol. 17, 384–389 (2022)
Majoranas, precursors, topological ???
Fe chains on Pb(110)
S. Nadj-Perge et al. Science, 346, 622 (2014)
Way forward: Better modelling
Parameter free
Includes proper geometry
Material specific

## Slide 8: Why is it difficult?
„semi-infinite” material
Surface nanostructure
Magnetism
Relativistic effects
Superconductivity (coherence length)
BULK
G = G
n+1
n
SSKKR code

## Slide 9
Local Green’s function MST:
What is the computational task?
z: complex energy, 16-500
I,I’ : layer index, = 20-100
L,L’: angular momentum, 9, 16
s,s’: spin, 2
a,b: electron, lyuk, 2
K|| : 250-10 000

## Slide 10
Calculate the spectrum of the QPI states
The Fourirer series coefficients gives the intensities in the spectrum
This is a sampling of the k space, average over different chains provide more k points
Shiba bands in Mn/Nb(100) chains

## Slide 11: Fe chain on Au covered Nb(110)

## Slide 12
DOS of Fe chains on Au covered Nb(110) at various spiraling angles
SOC=1
DOS: LDOS summed over
chain atoms
State is from F to AF
LDOS:
along the Fe atoms at E=0
E
Atomic position
…
…
…
…

## Slide 13
tiltott sáv
tiltott sáv
tiltott sáv
tiltott sáv
Band inversion reasoning
Artificial Fe atomic chains on Nb(110) covered by a Au ML
Difference between electron and hole parts of LDOS
band inversion
no band inversion
L. Schneider et al.
Nat. Phys. 17, 943 (2021)
The edge states are (most likely) Majoranas !

## Slide 14: Topological band structure and band inversion
See for example A. Bansil et al, arXiv:1603.03576
Colloquium: Topological band theory
A. Bansil, Hsin Lin, and Tanmoy Das
Rev. Mod. Phys. 88, 021004 – Published 29 June 2016
Topologically trivial phase

## Slide 15: Topological band structure and band inversion
See for example A. Bansil et al, arXiv:1603.03576
Colloquium: Topological band theory
A. Bansil, Hsin Lin, and Tanmoy Das
Rev. Mod. Phys. 88, 021004 – Published 29 June 2016
Topological phase

## Slide 16: Bulk-edge correspondence
Topological
Phase 1
Topological
Phase 2
Something special at the boundary
What defines topology in the magnetic wire/superconductor system?

## Slide 17
LDOS
Majorana Zero Mode at the boundary of topological trivial and topological region
U
V
U
V
U
V
V
U
V
U
V
U
V
U
V
U
V
U
V
U
U
V
U
V
Zero energy state at the transition
(50%)
CDOS

## Slide 18
Stability of MZMs against white noise
Artificial Fe atomic chains
A. Lászlóffy et al., Phys. Rev. B 108, 134513 (2023)

modify spin directions randomly
max= 60o
max= 90o
max= 120o
max= 172o
0= 100o
MZMs

## Slide 19
Fe adatoms on IrNb(110), ferromagnetic state
0⁰ (F)
90⁰
180⁰ (AF)
-90⁰
[110](x)
[001](y)
[111](xy)

## Slide 20
Mn adatoms on IrNb(110), ferromagnetic state
0⁰ (F)
90⁰
180⁰ (AF)
-90⁰
[110](x)
[001](y)
[111](xy)

## Slide 21: Fully relaxed spirals, ground state and topological analysis
Relaxing the chains both spatially and magnetically results in surprisingly many
number of spirals. However very few has Majorana edge states.
Trivial | Gap
Topological | Gap with MZM
Other | Maybe longer chain?
Filled | Entire gap is filled
Overlayers: Ag, Re, Ir Chains: Mn, Fe, Co, Cr

## Slide 22: Simulation of chain AND tip
Palotás, Mándi, Hofer,
Frontiers of Physics 9, 711 (2014)
Current:

## Slide 23
    HUN-REN Wigner Research Centre for Physics
    András Lászlóffy
    Krisztián Palotás
    Levente Rózsa
    Kyungwha Park
    University of Hamburg
    Philip Beck
    Lucas Schneider
    Jens Wiebe
    Roland Wiesendanger
    Jannis Neuhaus-Steinmetz
    Thore Posske
    Budapest University of Technology
    and Economics
    Bendegúz Nyári
    László Szunyogh
Star of the show:
KOMONDOR

## Slide 24
Runtime is 8.6X faster for the GPU code (14.5 PFlop/s)
Energy consumed Is 7.3X less
  GPU accelerated code consumed 3,500 kW-hr
  CPU only code consumed 25,700 kW-hr
Power consumption traces for identical WL-LSMS runs with 1024 Fe atoms on 18,561 Titan nodes (99% of Titan)
Power Efficiency on Titan (ORNL)
M. Eisenbach et al. CPC 212, 2 (2017)
Notes: WL-LSMS effectively utilizes compute resources on both x86-only and GPU-accelerated implementations.
The GPU accelerated run aggregate was 3,526.72kW-hr
the CPU only run aggregate was 25,692.12kW-hr.

## Slide 25
Summary
We successfuly generalised the SKKR method to solve the Kohn-Sham-Dirac Bogoliubov-deGennes equations for embedded clusters
Studied chariousains on Nb(110) superconductor surface
  We found an internal topological gap within the Shiba bands at a wide range of spiraling angles.
  Here some zero bias peaks còuld be observed on the edge atoms.
  A special kind of triplet states are indicated by the order parameter.
Indications point towards a Majorana state from first principles
The Majorana states are robust against perturbation in the magnetization direction of the spiral
Easy to get Quasi-Majorana states
Overlayer systems may support Majorana’s on rear occasion
Thank you for your attention!

## Slide 26
For Inhomogeneous superconducting materials:
Solution with band theoretical methods:
implementation in Relativistic SKKR
Superconducting order parameter, Charge density:
BULK
Surface and interface systems
semi-infinite, inhomogeneous
Semi-infinite Green function in MST (NO supercell)
Density functional Theory for superconductors
Oliviera, Gross, Kohn, Phys. Rev. Letters, 60 2430 (1988)
Suvasini, Temmerman, Győrffy, Phys. Rev. Letters, 48 1202 (1999)
Methodology
Impurity systems
Green’s function embedding
Surface impurities, nanostructures (NO supercell)
Conventional or Unconventional
pairing can be included
Four component Dirac Spinor operator Ѱ
K. Capelle and E. K. U. Gross, Phys. Rev. B 59, 7140 (1999), Phys. Rev. B 59, 7155 (1999)
Csire et al, Phys. Rev. B 97, 024514 (2018)

## Slide 27
The Lutchyn-Oreg wire
s=1/2 particles
Rashba SOC
Zeemann
splitting
s-wave pairing
R. M. Lutchyn et al, Phys. Rev. Lett. 105, 077001 (2010)
Y. Oreg et al, Phys. Rev. Lett. 105, 177002 (2010)
Needs irrealistic parameters (Δ t ) to get realistic observables (localization length of MZM)
Supercondutor surface is not included (Δ is on the wire)
J. Li et al., Phys. Rev. B 90, 235433 (2014)
L. Schneider et al. Nat. Commun. 11, 4707 (2020)

## Slide 28
3D-WKB-STM method:
Orbital- and spin-dependent electron tunneling
Palotás, Mándi, Hofer,
Frontiers of Physics 9, 711 (2014)
Transmission
non-spin-polarized part
spin-polarized part
Atom-
superposition
approach:
Sa
In effect
3D-WKB
1D-WKB
transitions
Current:
Transmission:
χ: electron orbital character: s, pz, dz2, etc.
nsβ , nTγ: orbital-decomposed atom-projected
charge DOS (↑+↓)
msβ , mTγ: orbital-decomposed atom-projected
magnetization DOS (↑-↓) vector
Mándi and Palotás, Appl. Surf. Sci. 304, 65 (2014)
Palotás et al., Phys. Rev. B 86, 235415 (2012)

## Slide 29: Computer experiments to prove Majorana behaviour

## Slide 30: The BdG equations
We turn to the Bogoliubov de Gennes equations:
Elektron-like
hole-like
Description of non-homogeneous superconductor-superconductor systems
non-homogeneous superconductor-normal metal systems
non homogeneous superconductor-magnet systems

## Slide 31: Mn chain on Ta(110)
DOS
LDOS(ɛ=0)
ꭕs
ꭕT

## Slide 32
Majorana bound states in ferromagnetic YSR chains
(5) S. Nadj-Perge et al., Science 346, 602 (2014)
    YSR states overlap, hybridize and form bands in a magnetic atomic chain on a superconductor
    Majorana bound states close to inside the p-wave gap opened in the YSR band
    Majorana states localized at the ends of the chain, YSR states extend over the chain

## Slide 33
Quasi Majorana Bound States (QMBS) aka „Fake” Majorana
Perturbation of the local exchange
field at the last atoms of a chain in
a non-topological regime: Bexc=0.95 B0exc
Topologically trivial order parameter ꭕs(ɛ)
LDOS shows edge state