## Slide 1: Nano-containers and nano-scaffolds
Katalin Kamarás
Institute for Solid State Physics and Optics,
Wigner Research Centre for Physics,
Hungarian Academy of Sciences, Budapest

## Slide 2: Wigner Research Centre for Physics Advanced Structural Laboratory
FIR/MIR
MIR/NIR
Near field/SNOM
Photoluminescence

## Slide 3: Hybrid structures from nanotubes
peapod
adsorbed organic molecule
  Nano-containers
  van der Waals interaction inside
  nanosize reaction vessel
  packaging of unstable, toxic molecules
  Nano-supports
  π-π interaction on surface
  increased solubility
  “glue”
D. Eder:
Chem. Rev. 110,
1348 (2010)
exceptional properties of nanotubes:
  mechanical stability
  electric conductivity
organic components:
  selectivity
  function
Incorporation of functional units

## Slide 4: Coronene@SWNT
coronene both encapsulated and adsorbed
adsorbed coronene dissolves in toluene
ATR-IR

## Slide 5: Reactions inside nanotube
low-temperature filled nanotubes: no side reactions on adsorbed molecules
surface can be cleaned by toluene washing
adsorbed molecules do not obscure encapsulated ones
Can we stop the process at the nanoribbon stage?
A.V. Talyzin, I.V. Anoshkin,
A.V. Krasheninnikov, R.M. Nieminen,
A.G. Nasibulin, H. Jian, E.I. Kauppinen:
Nano Lett. 11, 4352 (2011)

## Slide 6: Following reactions by Raman spectroscopy
Resonance with nanoribbons:
500, 700, 900 ºC
Resonance with nanoribbons:
700, 900 ºC
DWNT formation: 1250 ºC

## Slide 7: Lead halide perovskites
E. Mosconi, A. Amat, Md.K. Nazeeruddin, M. Grätzel, F. De Angelis:
J. Phys. Chem. C 117, 13902 (2013)
T. Baikie, Y. Fang, J.M. Kadro, M. Schreyer, F. Wei,
S.G. Mhaisalkar, M. Grätzel, T.J. White:
J. Mater. Chem. A 1, 5628 (2013)
the solar cells of the future

## Slide 8: Lead halide perovskites: nanoscale
E. Horváth, M. Spina, Zs. Szekrényes, K. Kamarás, R. Gaal, D. Gachet, L. Forró:
Nano Lett. 14, 6761-6766 (2014)
CH3NH3PbI3 nanowires with 50 – 200 nm diameter

## Slide 9: Perovskite nanowires: using carbon nanotubes as scaffolds
CH3NH3PbI3 nanowire
Transparent CNT film
M. Spina, B. Náfrádi, H.M. Tóháti, K. Kamarás, E. Bonvin, R. Gaal,
L. Forró, E. Horváth:
Nanoscale 8, 4888 (2016)
strong
transparent
chemically inert?
yes

## Slide 10: Photoinduced spectral changes
Presented as
Illumination by 633 nm light
Carbon nanotubes are
ideal hole transport layers!

## Slide 11: Boron nitride nanotubes
Both covalent and van der Waals bonds have ionic character
electrons are less delocalized
h-BN is an insulator with a bandgap of 6 eV
folding
BNNT nanotube
Z. Gao et al.: Nanobiomedicine, 2014, 1:7.

## Slide 12: Electron microscopy of BNNT
external diameter 5.62 ± 2.16 nm
internal diameter 2.61 ± 1.05 nm
interlayer spacing 0.32 nm (h-BN)
Samples: BNNT LLC
Measurements: Andrei N. Khlobystov

## Slide 13: Filling of BNNT
BNNT as is
shortening (~2 μm  ~500 nm)
opening
purification (ammonia, annealing)
BNNT open
C60@BNNT
sublimation filling 600 C
W. Mickelson, S. Aloni, W.-Q. Han, J. Cumings, A. Zettl: Science 300, 467 (2004)

## Slide 14: Microscopy of BNNT peapods
A.N. Khlobystov, D.A. Britz, J. Wang, S.A. O’Neil, M. Poliakoff, G.A.D. Briggs: J. Mater. Chem. 14, 2852 (2004)
zigzag
two-molecule layer
W. Mickelson, S. Aloni, W.-Q. Han, J. Cumings, A. Zettl: Science 300, 467 (2004)
linear chain

## Slide 15: Infrared spectra of peapods
CNT
Infrared spectra
of C60 shielded
BNNT
C60 vibrations can be
clearly seen
C60 retains Ih symmetry
(no splitting of
vibrational bands)
free rotation at room temperature

## Slide 16: Formation of inner nanotube
electron beam
W. Mickelson, S. Aloni, W.-Q. Han, J. Cumings, A. Zettl: Science 300, 467 (2004)
laser 355 nm
annealing 1200 C

## Slide 17: “Towards the world’s smallest coaxial cable”
K.E. Walker, G.A. Rance, Á. Pekker, H.M. Tóháti, M.W. Fay, R.W. Lodge, C.T. Stoppiello, K. Kamarás, A.N. Khlobystov:
Small Methods, published online, DOI: 10.1002/smtd.201700184

## Slide 18: Collaborators
Funding:
VEKOP 2.3.2-16-2016-00011
VEKOP 2.3.3-15-2016-00001
NK 105691
SNN 118012
EU PITN-GA 2008-215399
FINELUMEN
Bea Botka
Ákos Botos
Melinda Füstös
Áron Pekker
Zsolt Szekrényes
Hajnalka M. Tóháti
Miklós Veres
Endre Horváth
Bálint Náfrádi
László Forró
Kate E. Walker
Graham A. Rance
Thomas W. Chamberlain
Andrei N. Khlobystov